## Slide 1: Spring Design II
ME 3320 Lecture 20

## Slide 2: Extension or Tension Springs
Extension springs are wound tightly with preloaded coils and provided with hooks or loops by bending out the last coils.
Hooks and loops are in bending, have high stress concentration and often fail.
An option is to screw a threaded plug into the last several coils and apply the force to the plug to avoid the loop problems.
Drawbar springs avoid these problems by using a compression spring to provide a tension force

## Slide 3: Helical Extension Springs

## Slide 4: Spring Index

## Slide 5: Deflection and Spring Rate

## Slide 6: Stress in Extension Springs

## Slide 7: Stresses in Hooks and Loops

## Slide 8: Stresses in Hooks and Loops

## Slide 9: Spring Surge
Dynamic excitation near the spring’s natural frequency will cause violent surging and failure
Surge frequency is calculated the same way as for helical compression springs

## Slide 10: Static Yield Strength of Spring Wire in Bending and Torsion

## Slide 11: Dynamic Yield Strength of Spring Wire in Bending and Torsion

## Slide 12: Torsional Endurance Limit of Spring Wire
High-strength materials 0ver 200 kpsi Sut tops-out in endurance strength.
Spring wire below 10-mm dia is in this category.
Zimmerli reports that all steel wire < 10 mm dia, loaded with repeated stress has:
Note that this not a fully reversed endurance limit.

## Slide 13: Effect of Spring Index

## Slide 14: Torsion Springs
These springs provide a torque, but are stressed in bending
(Note that compression and extension springs provide a force abut are stressed in torsion.)

## Slide 15: Number of Coils

## Slide 16: Deflection & Spring Rate in Torsion Springs

## Slide 17: Coil Closure

## Slide 18: Stress Concentration in Torsion Springs

## Slide 19: Coil Stresses in Torsion Springs

## Slide 20: Material Strengths – Torsion Springs
We are in the unusual situation of having data for torsional fatigue strength, and must convert it to an equivalent bending fatigue strength.

## Slide 21: Safety Factors for Torsion Springs
Static
Fatigue

## Slide 22: Belleville Spring Washers

## Slide 23: Belleville Force-Deflection Functions

## Slide 24: Belleville Force-Deflection Curves

## Slide 25: Mounting Details to Allow Over-Center Operation

## Slide 26: Percent Error in Force Around Center Position of a Constant Force Belleville

## Slide 27: Stress in Belleville Washers

## Slide 28: Stacking Bellevilles
Bellevilles have small deflections.
Can stack in series to increase y.
If stack in parallel, forces add.
Are stiff springs so give high loads.
Often used as die springs.
Package very compactly.

## Slide 29: Examples
Study Examples 14-5, 14-6, and 14-7