## Slide 1: Demos
Pitted Gears
Milled and Ground cams

## Slide 2: Wear and Surface Fatigue
ME 3320 Lecture 15
R. L. Norton

## Slide 3: Types of Wear
Adhesive
Abrasive
Erosion
Corrosion
Surface fatigue

## Slide 4: Surface Finish

## Slide 5: Measuring Surface Finish

## Slide 6: Ra and Rq are not enough

## Slide 7: Real Area of Contact

## Slide 8: Adhesive Wear
Also called scoring, scuffing, or galling
Reduced by mating incompatible materials
Reduced by lubricant or contaminants

## Slide 9: Abrasive Wear

## Slide 10: Abrasion Resistant Materials

## Slide 11: Corrosion Wear

## Slide 12: Fretting

## Slide 13: Surface Fatigue

## Slide 14: Hertzian Stress
Hertz discovered that materials in contact
  Have normal stresses in three dimensions
  These occur on the axes normal to and orthogonal within the tangent plane of contact
  These will also be the principal stresses
There are three cases of interest
  General contact – any shaped surfaces
  Cylindrical contact – cyl. on cyl. or cyl. on plane
  Spherical contact – ball on ball or ball on plane
The second 2 are special cases of the first

## Slide 15: Surface Contact Creates a “Patch”

## Slide 16: Three Types of Surface Contact
Spherical, Cylindrical, General

## Slide 17: Static Sub- Surface Stresses
Hertzian normal stresses – Spherical contact
Maximum shear stress is below the surface

## Slide 18: Dynamic Sub- Surface Stresses

## Slide 19: Dynamic Sub- Surface Stresses

## Slide 20: Fatigue Cracks

## Slide 21: Roller Cam-Followers

## Slide 22: Stress Concentration in Surface Contact

## Slide 23: Surface Fatigue Strength
There is no “knee” in the strength-life curve for surface loading
So, all parts in surface fatigue will eventually fail – infinite life is not possible.
Nevertheless, very long lives can be achieved.
Example: Wheel bearings in cars often last 100,000 miles.
  At an average speed of 40 mph and a wheel radius of 1 foot a wheel bearing will rotate about 84 million times in 100,000 miles

## Slide 24: Surface Fatigue Strength
There is not much public data available on the strength of materials in surface fatigue
A famous study was done at United Shoe Machine Co. in the 1930s
This study lasted 24 years and ran various materials together under load to determine their surface fatigue life.
Some of these data are presented in your text.

## Slide 25: Surface Fatigue Strength Data
From 24 years of 24-hours a day, continuous testing of loaded rollers.

## Slide 26: Roller Bearing Life

## Slide 27: Summary
Surface contact has 3-D Hertzian stress.
Typically fails in surface fatigue by pitting and spalling.
Can fail by abrasion if in a dirty environment.
Good lubrication is preferred, but some joints are run dry (where lubricants might contaminate the product) risking possible adhesion failure.
Ideal case is to lubricate copiously with filtered oil (cooled if necessary).