## Slide 1: Fully Reversed Stress Notch Sensitivity Residual Stress
ME 3320 Lecture 10
R. L. Norton

## Slide 2: Notch Sensitivity and Fatigue Stress Concentration Factor

## Slide 3: Materials Have Notch Sensitivity

## Slide 4
Notch Sensitivity and Stress Concentration
Stress concentration factors in fatigue are different:
Are a function of geometric stress concentration and the material’s notch sensitivity q
Use these stress concentration factors for fatigue:
Notches introduce stress-concentrations.

## Slide 5
Stress concentration factors in fatigue:
Fatigue Stress Concentration Factor
Notches and stress concentrations
Theoretical (static) stress-concentration factor:
Neuber’s constant (depends on the value of the ultimate tensile strength of the material used). See, for example, Tables 6-6, 6-7, and 6-8
Notch sensitivity factor:
= Neuber’s constant

## Slide 6
Fatigue failure
Designing for HCF

## Slide 7: Residual Stress

## Slide 8: Residual Stress
Stress “built-in” to a part at manufacture or at assembly.
Can “protect” against fatigue failure if done right or can make situation worse if wrong.
All fatigue failures are due to tensile stress.
  Residual tensile stresses promote failure.
By building in residual compressive stress, can shift the failure threshold.
  Any applied tensile stress has to first “undo” the residual compression before the part knows it’s being tensile stressed.

## Slide 9: Creating Beneficial Residual Stress
In bending and torsion, stress is max at the surface
Thermal treatment
  Through hardening leaves tensile residual stress in the surface – not good
  Case hardening leaves compressive stress in the surface – good
Surface treatment
  Cold working – hammering, drawing, rolling
  Shot peening
Prestressing
  Overstress and yield part once in same direction as will be loaded in service – only works for non-reversed loading

## Slide 10: Case Hardening - Residual Stress

## Slide 11: Effect of Shot Peening

## Slide 12: Prestressing

## Slide 13: Sources of Harmful Residual Stress
Residual surface tensile stress is induced by
  Through hardening
  Grinding
  Welding
  Loading beyond yield point in direction opposite to applied stress direction before putting part in service

## Slide 14
Residual stresses introduced during welding caused crack initiation
Residual Stress due to Welding
Residual stresses are built-in or introduced (typically during manufacturing) to an unloaded part either inadvertently or deliberately.
Tensile residual stresses can be the cause of crack initiation and therefore promote fatigue failure.
Source: ASM International
Example: rotary dryer. Welding lifters to a rotary shell

## Slide 15: Designing for Fully Reversed Stress

## Slide 16
Four Fatigue Design Categories

## Slide 17: Types of Loading
We will first design for fully reversed loading

## Slide 18: Fatigue Strength in the Fully Reversed Stress Case
Steel
Plastics
Aluminum
Strength decreases with number of fully-reversed cycles

## Slide 19: Determine a Corrected Fatigue Strength

## Slide 20: Determine the Alternating Stress on the Part
Fully reversed load of 1000 lb (amplitude, therefore, is 500 lbs)
Life of about 10 9 cycles
Material: 1040 steel/machined
Operating conditions: room temp.
See Example 6-4
= 500 lb

## Slide 21
= 500 lb

## Slide 22
Example 6-4: fully-reversed bending
Find the Geometric Stress Concentration Factor Kt

## Slide 26: Observations
Had to make assumptions about size, material, etc.
First attempt was unsuccessful. This is to be expected in design!
Iteration is usually required in design.
If you don’t use an equation solver for design problems, you will waste time recalculating and make mistakes in the process. (No pity from me!)
Set the problem equations up in a software package and use its ability to quickly iterate to a solution by playing “what if” with your assumed values for design parameters.
TKSolver is the best “iterator” of all the packages as it can be backsolved for a desired outcome.