## Slide 1: Fluctuating Stress
ME 3320 Lecture 11
R. L. Norton

## Slide 2
Four Fatigue Design Categories

## Slide 3: Effect of Mean Tensile Stress on Fatigue Strength
Steel
Alum.

## Slide 4: Effect of Mean Comp-ressive Stress on Fatigue Strength

## Slide 5
Fatigue failure
Designing for HCF: fluctuating uniaxial stresses
Gerber parabola:
(Fits experimental data:
useful to study failed parts)
Soderberg line:
(Overly conservative theory)
Modified-Goodman line:
(Conservative theory)

## Slide 6
Fatigue failure – Fluctuating Stress
Modified GoodmanSurface – with knee

## Slide 7
Fatigue failure
Augmented modified Goodman-diagram
Area in “gray” is the “safe-zone”

## Slide 8
Fatigue failure
Stress-concentration factors in fluctuating stresses
Note that component may “yield” locally

## Slide 9
Fatigue failure
Stress-concentration factors in fluctuating stresses
Mean stress fatigue-concentration factor:
See figures at the bottom of previous page

## Slide 10
Fatigue failure
Safety factors in fluctuating stresses: Cases 1 and 2

## Slide 11
Fatigue failure
Safety factors in fluctuating stresses: Cases 3 and 4

## Slide 12: Fluctuating Bending (Ex 6-5)

## Slide 13: Fluctuating Bending (Ex 6-5)

## Slide 20: General Approach to HCF Design

## Slide 22
Fatigue failure
Designing for HCF. Review example: multiaxial fluctuating stresses
MASTER - Example 6-6: fatigue under multiaxial fluctuating stresses. Determine safety factors for the tube shown in the figure
Comment: use MathCad example to perform design iterations (file is included in the CD-ROM that came with your textbook)
OD
Fluctuating load
Finite life of about 6x10 7 cycles
Material is 2024-T4: Sy=47,000 psi, Sut=68,000 psi
Operating conditions: air at max. temperature of 120 oF
Force varies from F = 340 to -200 lb
Notch radius at the wall is 0.25 in
Theoretical stress-concentration factor (at the wall) for bending and shear are Kt = 1.7 and Kts = 1.35, respectively