## Slide 1: Fatigue Failure Theory
ME 3320 Lecture 8
R. L. Norton

## Slide 2
Fatigue failure theories
Mechanisms of fatigue failure
Fatigue failures always begin at a crack
  Cracks may be present in raw material used for fabrication (crystallographic defects; inclusions; etc.)
  Cracks may be introduced during fabrication
  Cracks develop over time due to cyclic loading (& corrosion)
  Cracks develop around stress concentrations
Shaft with keyway
Shaft failed in fatigue.
Crack initiated at keyway
Failure due to rotating bending

## Slide 3
Fracture Mechanics Stages of crack propagation
There are three stages of fatigue failure:
  Crack initiation: Region I
  Crack propagation: Region II
  Sudden fracture: Region III
Crack growth rate
  Valid only in Region II (defined by the Paris equation):
Region
Region
Region
The Paris Equation:

## Slide 4: Crack Growth Striations

## Slide 5
Fatigue failure
Important definitions and considerations
Fatigue failure models
  Stress-life (S-N) approach: used in HCF. Stress based model. In this model, we seek to obtain designs in which the maximum cyclic stress induced in the component is lower than the fatigue strength and/or endurance limit of the material used
  Strain-life (-N) approach: used in LCF. Strain based model. Used when the cyclic load is high enough to cause local yielding. Also used when cyclic and thermal loads are considered
  Linear-elastic fracture-mechanics (LEFM) approach: used in LCF and finite life situations. Used to design and model in the crack propagation stage (Region II). Used when the cyclic load is high enough to cause the formation of cracks
Fatigue regimes
  Low-cycle fatigue (LCF)
  High-cycle fatigue (HCF): when number of cycles, N > 103 cycles.
  Crankshafts of cars rotate about 2.5x108 cycles in 100,000 miles
Our design should minimize stress concentrations -- to minimize effects of cracks

## Slide 6
Fatigue failure
Important definitions
Stress range:
Alternating stress component:
Mean stress component:

## Slide 7
Fatigue failure
Important definitions
Wohler strength-life or S-N diagram
Theoretical or uncorrected fatigue strength:
Theoretical or uncorrected endurance limit:

## Slide 8
Fatigue failure
Important definitions
Materials with a “knee” in the S-N curve:
Many low-strength carbon and alloy steels
Some stainless steels
Irons
Molybdenum
Titanium, and some polymers
Knee typically appears at nearly 106 cycles
Endurance limit at 106 cycles is typically used
Materials without a “knee” in the S-N curve:
Aluminum, magnesium, copper
Nickel alloys
Some stainless steels
High-strength carbon and alloy steels
Fatigue strength at 5108 cycles is typically used

## Slide 9
Fatigue failure
Experimental observations: materials with a “knee”
Wrought steel, Sut < 200 ksi
“Knee”
Endurance limit

## Slide 10
Fatigue failure
Experimental observations: materials without a “knee”

## Slide 11: How Determine Fatigue Strength?
Test, Test ,Test

## Slide 12: What if have no test data?
Make your best estimate based on:
  Theory
  Historical test data
  Experience
  Conservative engineering practice

## Slide 13
Estimating fatigue failure criteria
Based on experimental observations (bending, torsion, axial fatigue testing)
For steels:
For irons:
For aluminums:
Some materials with a “knee”
Some materials without a “knee”
For copper alloys:

## Slide 14
Fatigue failure
Correcting theoretical fatigue data
Materials with a “knee.” Correcting function:
Correction factors:
Other factors may need to be added… depending on the type (& service) of components being designed...
Materials without a “knee.” Correcting function:
at 5 x 10 8 cycles

## Slide 15
Fatigue failure
Correcting theoretical fatigue data
Loading effects (correction):

## Slide 16
Fatigue failure
Correcting theoretical fatigue data
Size effects (correction; cylindrical parts):
Size effects (correction; non-cylindrical parts):

## Slide 17
Fatigue failure
Correcting theoretical fatigue data
Surface effects (correction):

## Slide 18
Fatigue failure
Correcting theoretical fatigue data
Surface effects (correction; Shigley and Mischke):

## Slide 19
Fatigue failure
Correcting theoretical fatigue data
Temperature effects (correction):

## Slide 20
Fatigue failure
Correcting theoretical fatigue data
Reliability effects (correction):
Standard deviation

## Slide 21
Fatigue failure
Correcting theoretical fatigue data
Once fatigue strength/endurance limit has been corrected… construct estimated (corrected) S-N diagram
Corrected
Corrected
Materials with a “knee”
Materials without a “knee”
Corrected S-N diagram

## Slide 22
Fatigue failure
Creation of estimated S-N diagrams
Fatigue strength at 103 cycles:

## Slide 23
Fatigue failure
Creation of estimated S-N diagrams
Curve fitting of model (HCF-high cycle fatigue):
at 5 x 10 8 cycles

## Slide 24: Other Factors to Consider
Electroplating reduces fatigue strength
Environment
  Hydrogen embrittles steel
  Sulfur embrittles steel
  Fresh water is bad, salt water is worse
    Causes corrosion fatigue – must test

## Slide 25
Fatigue failure
Study Example 6-1: Ferrous materials (with a “knee”)
Study Example 6-2: Nonferrous materials (without a “knee”)