## Slide 1: Spring Design I
ME 3320 Lecture 19

## Slide 2: Video
Spring Manufacturing courtesy of the Dominion Spring Co.

## Slide 3: Spring Types

## Slide 4: Spring Types

## Slide 5: Spring Connections

## Slide 6: Helical Compression Springs

## Slide 7: Deflection and Spring Rate

## Slide 8: Stress in Compression Springs

## Slide 9: Residual Stress – Setting & Peening
Beneficial residual stress can protect against fatigue failure.
For unidirectional (non-reversed) loading we can take advantage of this.
Overloading the part once in the direction of service loading will yield the material locally and leave beneficial residual stress.
When done to coil springs, it is called setting the spring.
The spring is designed longer than needed and deflected once to its shut height, yielding it to the desired free length.
Shot peening can also be used to good effect to improve fatigue life provided spring wire is large enough and coil spacing sufficient

## Slide 10: Service Loading
Coil springs should not be subjected to reversed loading.
Even if unset, the coils will have residual stress from the winding process.
Reversing their designed load pattern will cause premature failure.
This not this:

## Slide 11: Buckling
A coil spring in compression acts like a column and can buckle.
End conditions contribute as in columns.

## Slide 12: Spring Surge
Dynamic excitation near the spring’s natural frequency will cause violent surging and failure
Video of Spring Surge
Note typo correction

## Slide 13: Spring Materials

## Slide 14: Minimum Tensile Strength of Spring Wire

## Slide 15: Minimum Tensile Strength of Spring Wire
Fitted equation

## Slide 16: Minimum Strengths of Spring Wire
Fitted equation

## Slide 17: Torsional Static Yield Strength of Spring Wire

## Slide 18: Torsional Fatigue Strength of Spring Wire

## Slide 19: Torsional Endurance Limit of Spring Wire
High-strength materials 0ver 200 kpsi Sut tops-out in endurance strength.
Spring wire below 10-mm dia is in this category.
Zimmerli reports that all steel wire < 10 mm dia, loaded with repeated stress has:
Note that this not a fully reversed endurance limit.

## Slide 20: Goodman Diagram for Torsion

## Slide 21: Fatigue Safety Factor – Coil Springs

## Slide 22: Effect of Spring Index

## Slide 23: Examples
Study Examples 14-3 and 14-4