## Slide 1: Gear Design II
ME 3320 Lecture 18
R. L. Norton

## Slide 2
Spur Gears
Forces on pinion and gear sets – time-varying forces
Tangential force component:
Radial force component:
Resultant force:
Note: for contact ratios > 1, there exists a HIGHEST POINT OF SINGLE-TOOTH CONTACT (HPSTC)

## Slide 3: Gear Teeth Always Have Dynamic Loading Even if Applied Load is Constant
Gear teeth see both bending and surface stresses
Gears can be designed for infinite life against bending failure
Gears cannot be designed for infinite life against surface failure
There is no endurance limit for surface stress
They will eventually fail in surface fatigue by pitting and spalling
Inadequate or dirty lubrication can cause premature failure by adhesion or abrasion.
Automobile gears very rarely fail in the life of the vehicle unless abused in service.

## Slide 4
Spur Gears
Bending stresses (note that contact stresses are also generated)
Tooth is modeled as a Cantilever beam in bending:
Bending stresses:

## Slide 5
Spur Gears
Bending stresses
y
Gear tooth in
bending:
Bending stresses (Lewis’ equation):
Wt is the tangential force
pd is the diametral pitch
F is the face width
Y is the geometric factor (Lewis dimensionless geometric factor)

## Slide 6
Spur Gears
Bending stresses
F is face width (minimum face width is 3 to 5 times pc)
J is bending strength geometric factor (AGMA; Tables 11-8 through 11-15; pg. 716)
Kv is dynamic factor (depends on tangential velocity -- Figure 11-22; pg. 719)
Km is load distribution factor (to account for misalignments -- Table 11-16; pg. 720)
Ka is application factor (application dependent; “Shocks” -- Table 11-17; pg. 721)
Ks is size factor (similar concept as Equation 6.7b -- AGMA recommends value of 1)
KB is rim thickness factor (for gears made of rims and spokes -- Figure 11-23; pg. 721)
KI is idler factor (set to 1.42 for an idler gear and 1 for a non-idler gear)
AGMA bending stress equation:
U.S. specifications
SI specifications - m is the
metric module

## Slide 7
Spur Gears
Bending stresses (note that contact stresses are also generated)
Contact ratio between 1 and 2 (# of teeth in contact at a given time)
No interference between tips and roots
No teeth are pointed
There is nonzero backlash
Root fillets are standard
Friction forces are neglected (assumed good lubrication)
AGMA standard 2001-B88 is subject to following general constraints:

## Slide 8: Load Sharing

## Slide 9: AGMA Dynamic Factor

## Slide 10: AGMA Geometry Factor J

## Slide 11: Other AGMA Factors

## Slide 12: More AGMA Factors
Ks = Size factor
  Set to 1
KB = Rim thickness factor
  Set to 1 for a solid gear (no rim)
  See text for other cases
KI = Idler factor
  Set to 1 for a non-idler gear
  Set to 1.42 for an idler gear
    Idler sees fully reversed stress of twice the range of non-idler

## Slide 13: Surface Stress in Gear Teeth
Can design teeth to never fail in bending
But they will eventually fail in surface fatigue

## Slide 14: Elastic Coefficient Cp

## Slide 15: Surface Geometry Factor I

## Slide 16: Gear Materials
Cast Iron
Steel
Bronze
Nonmetallic
  Nylon
  Delrin
  Phenolic

## Slide 17: Gear Material Strengths
AGMA has done extensive testing to establish fatigue strengths for gear materials in both bending and surface fatigue.
These data were generated with proper size, geometry, surface finish, etc., and so are partially corrected fatigue strengths.
They are stated at 1E7 cycles (unlike other data at 1E6 or 5E8) and are at 99% reliability level.
The test load was fluctuating, containing the mean stress component, so these data can be compared directly to the alternating stress on the tooth.
A Goodman line analysis is not needed here as the strength data already are in the Goodman domain.

## Slide 18: Gear Bending Fatigue Strength
Tabular data are published (see Table 11-20)
Formulae are also defined based on Brinell hardness

## Slide 20: Correcting Gear Bending Fatigue
Note that these are different factors than in Chapter 6 because these data are based on 99% reliability not 50%
Reliability Factor

## Slide 21: Bending Strength Life Factor KL
Modifies strength based on your cycle life

## Slide 22: Gear Surface Fatigue Strength
AGMA has done extensive testing on gears
Tabular data are published (see Table 11-21)
Formulae are also defined based on Brinell hardness

## Slide 23: Gear Surface Fatigue Strength

## Slide 24: Correcting Gear Surface Fatigue
CT is the same as KT defined earlier
CR is the same as KR defined earlier

## Slide 25: Surface Strength Life Factor CL
Modifies strength based on your cycle life

## Slide 26: Hardness Ratio Factor CH

## Slide 27: Lubrication
Gears need lubrication
Oil bath is best
Grease lubrication is a poor substitute
Hypoid oils are needed where sliding component of velocity is high
  Hyperboloidal (hypoid) gears
  Wormsets

## Slide 28
Examples
Study Examples 11-4, -5, -6, -7