CASE STUDY 4C

Bicycle Brake Arm Factors of Safety

Problem	Choose appropriate material alloys to obtain a safety factor of at least 2 at critical points in the bicycle brake arm shown in Figures 3-9 and 5-21.

Given	The stresses are known from the previous Case Stydy 4B (p. 265).  The arm is cast-aluminum and the pivot pin is ductile steel.

Assumptions	Since the arm is a brittle material the modified-Mohr theory will be used for it.  The pin is ductile, so the distortion-energy theory will be used for it.

Solution	See Figures 3-9 and 5-21, M-Book CASE4C.doc and M-File Case4c.m.

1	The bending stresses at the inner and outer fibers of the arm were found in Case Study 4B, step 1, to be

SIGi = 162.6;    % MPa

SIGo = -190.4;   % MPa

For a safety factor of 2 at this point we need a material with an ultimate tensile strength of at least 333 MPa and a compressive strength of at least 381 MPa.

2	The stress on the left half of Section B-B is the sum of the bending stress and the axial tension stress and was found in Case Study 4B, step 2, to be

SIGhub = 25.4;   % MPa

This needs a material tensile strength of 51 MPa to have a safety factor of 2.

3	The bending stress at the outer fiber of the 23-mm side of the straight portion of the brake arm was found in Case Study 4B, step 3, to be

SIGy = 142.3;    % MPa

For a safety factor of 2 at this point we need a material with an Sut of at least 285 MPa.

4	Another possible failure point is the slot in the arm.   The tearout shear stress was found in Case Study 4B, step 4, to be

TAU = 18.3;      % MPa

For a uniaxial applied shear stress, the stresses are all in the first quadrant of Figure 5-9 and the modified-Mohr theory is identical to the maximum normal-stress theory.  The equivalent tensile stress is then twice the maximum shear stress which requires an ultimate tensile strength greater than 75 MPa for a safety factor of 2 in this case.

5	The worst case among the points calculated is the curved beam root in (1) above.  From the material properties data for cast-aluminum in Appendix C, we find that the 220 sand-casting alloy has an Sut of 331 MPa, which satisfies the requirement for a safety factor > 2 in this case.  This material has an elongation of 16%.

6	The 11-mm-dia pivot pin is subjected to a maximum bending stress of

SIGpin = 176.4;  % MPa

For a safety factor of 2, this requires a steel with a yield strength of at least 353 MPa.  An AISI 1040 steel has Sy = 372 MPa in the normalized condition.  When this alloy is hardened, quenched, and tempered at 800F, it will reach a yield strength of about 1300 MPa and give the desired safety factor.

7	Figure 5-21 shows a summary of the stresses at various critical points in the part.