EXAMPLE 10-2

Lubrication in a Crowned Cam-Follower Interface

Problem	A cam-follower system was analyzed for contact-patch geometry and contact stresses in Example 7-3 (p. 505).   Determine the film thickness parameter and the lubrication condition for a ground roller running against both a ground cam and a milled cam.

Given	The roller follower radius is 1 in with a 20-in crown radius at 90 deg to the roller radius.   The cam's minimum radius of curvature is 1.72 inches, in the direction of rolling.  It is flat axially.  It forms an elliptical contact patch with the cam.

Roller and cam radii in x-direction

R1x = 1.000; % in

R2x = 1.720; % in

Radius of cam to contact point

r = 3.920;   % in

Half dimensions of elliptical patch

a = 0.0889;  % in

b = 0.0110;  % in

Cam angular velocity

OMEGA = 18.85;   % rad/sec

Bulk oil temperature

T = 180;     % deg F

Surface roughness

Follower

Rq1 = 7e-6;      % in

Milled cam

Rq2m = 30e-6;    % in

Ground cam

Rq2g = 7e-6;     % in

Material properties

Follower

E1 = 30e6;   % psi

v1 = 0.28;

Cam

E2 = 30e6;   % psi

v2 = 0.28;

Applied load on joint

P = 250;     % lbf

Assumptions	Try an ISO VG 460 oil with an assumed specific gravity SG = 0.9.  The roller has 1% slip versus the cam.

SG = 0.90;

Find	The specific film thickness and lubrication condition for the assumed lubricant and the viscosity of lubricant required to obtain effective partial or full EHD conditions for each cam, if possible.

Solution	See M-Book Ex10-02.doc and M-File Ex10_02.m.

1	Figure 10-1 gives the viscosity of an ISO VG 460 oil as about

ETAo = 6.5e-6;   % reyn (= lbf sec / in2)

at 180 deg F.

2	Find the mass density ρ of the oil from the given specific gravity SG of the oil and the weight density of water of γ = 0.03611 lbf in-3 and blob = lbf sec2 in-1.

GAMMA = 0.03611; % lbf / in3

g = 32.174 * 12 % in / sec2

RHO = SG * GAMMA / g    % lbf s2 / in4 = blob / in3

g =

386.0880

RHO =

8.4175e-005

3	Find the approximate pressure-viscosity exponent α from equation 10.15b.

ALPHA = 7.74e-4 * (ETAo/(RHO*1e4))^0.163

ALPHA =

1.1362e-004

4	Find the effective radius from equation 10.17a.

Rprm = 1/((1/R1x)+(1/R2x))  % in

Rprm =

0.6324

5	Find the effective modulus of elasticity from equation 10.17b.

Eprm = 2/(((1-v1^2)/E1)+((1-v2^2)/E2))  % in

Eprm =

3.2552e+007

6	Find the average velocity U.  The roller has 99% of the velocity of the cam.

U2 = r * OMEGA      % in / sec

U1 = 0.99 * U2      % in / sec

U = 0.5 * (U1 + U2) % in/sec

U2 =

73.8920

U1 =

73.1531

U =

73.5225

7	Find the ellipticity ratio = major/minor axis.  The minor axis is in the direction of rolling in this case.

PSI = a/b

PSI =

8.0818

8	Find the minimum film thickness from equation 10.16.

hmin = 3.63*Rprm*(ALPHA*Eprm)^0.49 *...

((ETAo*U)/(Eprm*Rprm))^0.68 * (1-exp(-0.68*PSI)) *...

(P/(Eprm*Rprm^2))^-0.073 % in

hmin =

1.6613e-005

9	Convert this minimum value at the exit to an approximate thickness at the center of the contact patch with equation 10.14b.

hc = (4/3)*hmin     % in

hc =

2.2151e-005

10	The specific film thickness values for each cam can now be found from equation 10.14a.

Ground cam:

LAMDAg = hc / sqrt(Rq1^2 + Rq2g^2)

LAMDAg =

2.2376

Milled cam:

LAMDAm = hc / sqrt(Rq1^2 + Rq2m^2)

LAMDAm =

0.7191

which indicates that the milled cam is in boundary lubrication and the ground cam is in partial EHD with the specified oil. These are common conditions for ground or milled cams, respectively, running against a ground roller-follower.

11	To determine what viscosity of oil would be needed to put each system into partial or full EHD condition, the model was solved for a range of possible h0 values from 0.5 to 16 µreyn as shown in Figure 10-1 at 180 deg F.  A plot of the results in Figure 10-16 shows that an oil with ?0 >= 14 ?reyn is needed to put this ground cam into full EHD and that an oil with η0 > 10 µreyn will get this milled cam to Λ > 1 and into the low end of the mixed-partial EHD lubrication regime.  But, none of the oils shown in Figure 10-1 can provide Λ > 4 for full-film EHD with the milled cam.