EXAMPLE 13-1

Constructing the S-N Diagram for a Spring Wire Material

Problem	Create the torsional-shear S-N diagrams for a range of spring-wire sizes.

Given	ASTM A228 music wire, unpeened.

Assumptions	Three diameters will be used: 0.010 in (0.25 mm), 0.042 in (1.1 mm), and 0.250 in (6.5 mm).

d1 = 0.010;  % in

d2 = 0.042;  % in

d3 = 0.250;  % in

Solution	See Figure 13-15, M-Book Ex13-01.doc and M-File Ex13_01.m.

1	The tensile strength of each wire size is found from equation 13.3 in combination with the coefficient and exponent from Table 13-4 for this material.

Sut1 = 184649 * d1^-0.1625  % psi (assumes d1 [=] inches)

Sut2 = 184649 * d2^-0.1625  % psi (assumes d2 [=] inches)

Sut3 = 184649 * d3^-0.1625  % psi (assumes d3 [=] inches)

Sut1 =

3.9025e+005

Sut2 =

3.0908e+005

Sut3 =

2.3130e+005

2	These values are converted to shear strengths at 1000 cycles using equation 13.13:

Sms1 = 0.6 * Sut1   % psi

Sms2 = 0.6 * Sut2   % psi

Sms3 = 0.6 * Sut3   % psi

Sms1 =

2.3415e+005

Sms2 =

1.8545e+005

Sms3 =

1.3878e+005

3	The torsional fatigue strengths Sfw at three values of N are provided as percentages of the tensile strength in Table 13-7 for unpeened A228 music wire.

N = 1e5;

Sfw1 = 0.36 * Sut1  % psi

Sfw1 =

1.4049e+005

N = 1e6;

Sfw2 = 0.33 * Sut2  % psi

Sfw2 =

1.0200e+005

N = 1e7;

Sfw3 = 0.30 * Sut3  % psi

Sfw3 =

6.9391e+004

These values are plotted in combination with the result from equation 13.13 to generate the S-N curves.

4	Figure 13-15 shows the S-N curves.  There are two separate portions to each S-N curve: the 1E3 ≤ N ≤ 1E5 segment and the segment for N ≥ 1E5.  The unpeened wire endurance limit for infinite life Sew is also shown at 45 000 psi (equation 13.12).

5	If desired, any of these S-N curves can be fitted to an exponential equation (Eq. 6.10) by the method shown in Section 6-6.  Evaluating the coefficients and exponents separately for the two pieces of the S-N curve allows the estimated wire fatigue strength Sfw to be easily found for any number of cycles.

6	It is important to remember that the Sfw data in Table 13-7 are for a repeated-stress state, not a fully reversed stress condition, which means that this S-N diagram is taken at some point along the σm axis in Figure 6-42.