EXAMPLE 11-7

Material Selection and Safety Factor for Spur Gears

Problem	Select suitable materials and calculate the safety factors for both bending and surface stresses in the 3-gear train from Examples 11-4, 11-5 and 11-6.

Given	Stresses from Examples 11-5 and 11-6:

Bending subscripted with "b", Surface with "c".

Pinion

SIGbp = 9.518e3;  %psi

SIGcp = 113.3e3;  %psi

Idler

SIGbi = 12.39e3;  %psi

SIGci = 90.7e3;   %psi

Gear

SIGbg = 6.828e3;  %psi

SIGcg = 53.40e3;  %psi

Pinion shaft speed

OMEGAp = 2500;    %rpm

Assumptions	The service life required is L = 5 years of one-shift operation.  All gears are steel.  Operating temperature is 200 deg F.

L = 5;   % yr

Solution	See M-Book Ex11-07.doc and M-File Ex11_07.m.

1	An estimate of the uncorrected bending-fatigue strength can be made from the curves of  Figure 11-25.  We will try an AGMA Grade 2 steel, through-hardened to HB = 250.  The uncorrected fatigue strength in bending is found from the upper curve of the figure to be

HB = 250;

Sprmfb = (6235 + 174*HB - 0.126*HB^2)   % psi

Sprmfb =

41860

2	This value needs to be corrected for certain factors using equation 11.24.

3	The life factor KL is found from the appropriate equation in Figure 11-24 based on the required number of cycles in the life of the gears.  The pinion sees the largest number of repeated tooth-loadings, so we calculate the life based on it.  First, calculate the number of cycles N for the required life of 5 years, one shift.

N = (OMEGAp * 60) * 2080 * L    % cycles

N =

1.5600e+009

The value of KL is found from

KL = 1.3558 * N^-0.0178

KL =

0.9302

4	At the specified operating temperature,

KT = 1;

5	The gear-material data are all taken at a reliability level of 99%.  This is satisfactory in this case, making

KR = 1;

6	The corrected bending-fatigue strength is then

Sfb = KL / (KT*KR) * Sprmfb     % psi

Sfb =

3.8937e+004

7	An estimate of the uncorrected surface fatigue strength can be made from the curves of Figure 11-27.  For an AGMA Grade 2 steel, through-hardened to 250HB, the strength is found from the upper curve of the figure to be

Sprmfc = 27000 + 364*HB         % psi

Sprmfc =

118000

8	This value needs to be corrected for certain factors using equation 11.25:

9	The life factor CL is found from the appropriate equation in Figure 11-26 based on the required number of cycles N found above.

CL = 1.4488 * N^-0.023

CL =

0.8904

10	Other factors include

CT = KT

CR = KR

CT =

1

CR =

1

11	Since the gears and pinion are of the same hardness material in this case,

CH = 1;

12	The corrected surface-fatigue strength is then

Sfc = (CL * CH) / (CT * CR) * Sprmfc    % psi

Sfc =

1.0506e+005

13	The safety factor against bending failure is found by comparing the corrected bending strength to the bending stress for each gear in the mesh:

Pinion

Nbp = Sfb / SIGbp

Nbp =

4.0908

Idler

Nbi = Sfb / SIGbi

Nbi =

3.1426

Gear

Nbg = Sfb / SIGbg

Nbg =

5.7025

which are acceptable.

14	The safety factor against surface failure is found by comparing the load that would produce a stress equal to the corrected surface strength to the actual load.  Because the surface stress is related to the square root of the load, the safety factor against a surface fatigue failure is found by comparing the square of the corrected surface strength to the square of the surface stress for each gear in the mesh:

Pinion-idler

Ncpi = (Sfc/SIGcp)^2

Ncpi =

0.8599

Idler-gear

Ncig = (Sfc/SIGci)^2

Ncig =

1.3418

which is low for the pinion-idler mesh.

15	A small change to the design will improve these.  Increasing the face width of the gears from the current 2.0 to 2.5 in (15/pd) reduces all stresses and gives new safety factors of

Pinion

Nbp = Sfb / SIGbp * 2.5 / 2

Nbp =

5.1135

Idler

Nbi = Sfb / SIGbi * 2.5 / 2

Nbi =

3.9282

Gear

Nbg = Sfb / SIGbg * 2.5 / 2

Nbg =

7.1281

Pinion-idler

Ncpi = (Sfc / SIGcp * sqrt(2.5 / 2))^2

Ncpi =

1.0748

Idler-gear

Ncig = (Sfc / SIGci * sqrt(2.5 / 2))^2

Ncig =

1.6772

16	These gears are very safe against tooth breakage and based on the assumptions and calculations, should have a 99% probability of lasting the required 5 years before pitting of the pinion or idler begins.