EXAMPLE 5-3

Failure of Cracked Materials Under Static Loading

Problem	A steel support strap designed to hold a 60 000 N static load in axial tension was accidently sawcut during production and now has an edge-crack in it.  Determine the safety factor of the original, uncracked strap based on yielding and its new "cracked" safety factor based on fracture mechanics.  How large could the crack get before it fails?  Would heat-treating the part compensate for the loss of strength due to the crack?

Given	Material is steel

Yield strength

Sy = 540;           % MPa

Fracture toughness

KC = 66;            % MPa m0.5

Strap length

l = 6;              % m

Strap width

b = 80;             % mm

Strap thickness

t = 3;              % mm

Load

P = 60000;          % N

Crack width

a = 10;             % mm

Assumptions	The load is static and the assembly is at room temperature.  The ratio a/b is < 0.13, which allows use of equation 5.14d.  The crack is completely through the thickness at one edge of the 80-mm width, similar to Figure 5-14c.

Solution	See M-Book Ex05-3.doc and M-File Ex05_03.m.

1	First calculate the nominal stress in the uncracked part based on total cross section.

Cross-section area

A = b*t             % mm2

A =

240

Nominal tensile stress

SIGnom = P/A        % MPa

SIGnom =

250

2		This is a uniaxial stress so is both the principal and the von Mises stress as well.  The safety factor against yielding using the distortion-energy theory is (equation 5.8):

von Mises stress

SIGprime = SIGnom   % MPa

SIGprime =

250

Factor of safety

Nvm = Sy/SIGprime   % no units

Nvm =

2.1600

3	The stress intensity K at the crack tip can be found for this case from equation 5.14d if the ratio a/b < 0.13:

a/b ratio

abRatio = a/b       % no units

abRatio =

0.1250

Stress intensity

K = 1.12 * SIGnom * sqrt(pi*(a/1000))      % MPa m0.5

K =

49.6287

4	The safety factor against sudden crack propagation is found from equation 5.15.

NFM = KC/K          % no units

NFM =

1.3299

Note that failure is now predicted to be sudden at a 33% overload at which point the nominal stress in the part is still below the yield strength.  This is too small a safety factor to allow the part to be used in the face of possible sudden fracture.

5	The crack size necessary for failure can be found approximately by substituting KC for K in equation 5.14b and solving for a.  The result is a crack of about

a = (1/pi) * (KC / (1.12 * SIGnom))^2 * 1000     % mm

a =

17.6857

Note however that the a/b ratio would now exceed that recommended for 10% accuracy with this equation.  A more accurate equation for this case could be obtained from one of the references if desired.

6	Assuming the steel has enough carbon to allow heat treatment, through hardening will increase the yield strength but the ductility and the fracture toughness KC will decrease making the part less safe against a fracture mechanics failure.