EXAMPLE 2-1

Determining Modulus of Elasticity and Yield Strength from Test Data

Problem	A standard specimen of medium-carbon steel was tested in tension and the data is given below.  Plot the data and determine the modulus of elasticity and 0.2% offset yield strength of the material from which the specimen was made.

Given	Gauge length

l0 = 50.80;  % mm

Specimen diameter

d0 = 12.78;  % mm

Tensile test data:

Load:

P = [0; 4.45; 8.90; 13.34; 17.79; 31.14; 37.37; 47.14; 47.92];  % kN

Deflection:

delta = [0; 8.16; 15.24; 26.40; 33.02; 58.42; 71.12; 152.4; 250.1];  % um

Assumptions	An approximation based on a cubic-spline fit to the data will be acceptable.

Solution	See Figure E2-1, M-Book file EX02-01.doc and Matlab file EX02_01.m.

1	Using equations 2.1a and 2.1b, calculate the engineering stress and strain in the specimen after first determining the specimen cross-section area.

Area

A0 = (pi*d0^2) / 4         % mm2

A0 =

128.2778

Stress

SIG = P / A0 * 1000;        % MPa

Strain

EPS = delta / l0 /1000;     % mm / mm

The calculated values of stress and strain are shown below.  The strain values are multiplied by 103 for convenience.

[SIG EPS*1000]

ans =

0         0

34.6903    0.1606

69.3807    0.3000

103.9930    0.5197

138.6834    0.6500

242.7543    1.1500

291.3208    1.4000

367.4836    3.0000

373.5642    4.9232

2	Use a cubic spline to define a stress-strain interpolation function.  Note, the [0; SIG; 0] notation specifies zero slope for the spline at each end of the curve. This prevents excess curvature in the spline fit at high strain values.

Range of strain

strain = 0:0.0001:EPS(9);    % mm / mm

Stress function (includes the spline interpolation)

stress = spline(EPS, [0; SIG; 0], strain);   % MPa

3	Use Matlab's regress function and the first 5 data points to find the slope of the stress-strain curve in the elastic region, which is the modulus of elasticity (equation 2.2).

Elastic range index

j = 1:5;     % first five data points are in linear region

Strain in elastic range

EPSe = EPS(j);    % mm / mm

Stress in elastic range

SIGe = SIG(j);    % MPa

Modulus of elasticity

E = regress(SIGe, EPSe) /1000     % GPa

E =

211.0090

4	Write an equation for the 0.2% offset line.

offset = E*(strain - 0.002) * 1000;    % MPa

5	The original data, the cubic-spline fit, and the offset line are plotted in Figure E2-1.

plot(EPS,SIG,'+',strain, stress,'-',strain,offset,'-')

xlabel('Strain')

ylabel('Stress (MPa)')

ylim([0 400])

Figure E2-1. Stress-Strain Data with 2% offset line

6	Find the intersection of the offset line and the cubic-spline fit. This is done by solving for the x value (strain value) that yields the same y value (stress value) for each equation. The two equations are first subtracted to eliminate the stress variable, then the fzero (find zero) function is used to find the strain value that causes the result to equal zero.

Strain guess value

x0=0.003;

x=fzero(@(x)spline(EPS,[0;SIG;0],x)-(E*(x-0.002)*1000),x0)

x =

0.0037

Stress value from spline curve

Sy = spline(EPS,[0;SIG;0],x)    % MPa

Sy =

367.3505

Stress value from offset curve (same value, computed as a check)

Sy = E*(x-0.002)*1000           % MPa

Sy =

367.3505