EXAMPLE 13-2

Creating the Modified-Goodman Diagram for a Helical Spring

Problem	Construct the Goodman line for the spring wire of Example 13-1.

Given	The required cycle life is N = 1E6 cycles.  Wire is 0.042-in (1.1- mm) dia.

d = 0.042;   % in

Assumptions	The torsional strengths and torsional shear stresses will be used on the Goodman diagram.

Solution	See Figure 13-16, M-Book Ex13-02.doc and M-File Ex13_02.m.

1	The material's ultimate tensile strength from Figure 13-3 or equation 13.3, converted to ultimate torsional strength with equation 13.4 using data from Table 13-4 allows one point on the Goodman line to be determined.

Sut = 184649*d^-0.1625  % psi

Sus = 0.67*Sut          % psi

Sut =

3.0908e+005

Sus =

2.0708e+005

This value is plotted as point A on the diagram in Figure 13-16 and in the following figure (on the x axis near 200).

plotX(1) = Sus/1000;

plotY(1) = 0;

plot(plotX,plotY,'o')

xlabel('mean shear stress TAUm (ksi)')

ylabel('alternating shear stress TAUa (ksi)')

xlim([0 250])

ylim([0 100])

Figure E13-02.1. Constructing the Modified-Goodman Diagram, part 1.

2	The S-N diagrams each provide one data point (Sfw or Sew depending on whether for finite or infinite life) on the modified-Goodman line for a material/size combina- tion in pure torsional loading.  The fatigue strength Sfw for that wire material and condition is taken from the S-N line of Figure 13-15 or calculated from the data in Table 13-7 as

N = 1e6;

Sfw = 0.33*Sut  % psi

Sfw =

1.0200e+005

The x and y intercepts are 0.707 Sfw = 72110 psi.  This is plotted as point B on the diagram in Figure 13-16.  Note that for infinite life the value of Sew from equation 13.12 would be plotted at B instead of this value of Sfw for a finite life.

plotX(2) = (0.5*Sfw)/1000;

plotY(2) = (0.5*Sfw)/1000;

plot(plotX,plotY,'o')

xlabel('mean shear stress TAUm (ksi)')

ylabel('alternating shear stress TAUa (ksi)')

xlim([0 250])

ylim([0 100])

Figure E13-02.2. Constructing the Modified-Goodman Diagram, part 2.

3	Note in Figure 13-16 that the wire fatigue strength Sfw is plotted on a 45 deg line from the origin to correspond to the test conditions of equal mean and alternating stress components (stress ratio R = τmin/τmax = 0).  Point B is then connected with the ultimate shear strength Sus on the mean-stress axis at point A to draw the Goodman line, which is extended to point C.

4	We can now find the value of the fully reversed fatigue strength (R = 1), which is point C on the diagram.  This value can be found from the equation for the Goodman line, defined in terms of its two known points, A and B:

m = -(0.5*Sfw) / (Sus - 0.5*Sfw)

Sfs = -m * Sus / 1000   % ksi

% alternative equation for Sfs

Sfs = 0.5 * (Sfw*Sus) / (Sus - 0.5 * Sfw) / 1000    % ksi

m =

-0.3267

Sfs =

67.6607

Sfs =

67.6607

5	The Gerber line is also plotted through points A and B.  Recall from Figure 6-16 (p.366) that the Gerber line is a better fit to experimental failure data for combined mean and alternating stresses.  Thus, the extrapolation of the Goodman line back to the τa axis in this case would seem to be nonconservative, and it is so for the shaded area in Figure 13-16.  However, this use of the Goodman line is conservative for stress ratios R >= 0 and its use is justified in this case because springs should always be loaded in the same direction.  Helical compression springs tend to have stress ratios between 0 and 0.8, which puts their stress coordinates to the right of the 45 deg line in the figure, where the Goodman line is more conservative than the Gerber line.

plotX(3) = 0;

plotY(3) = Sfs;

plot(plotX,plotY,'o-')

title('Modified-Goodman Diagram')

xlabel('mean shear stress TAUm (ksi)')

ylabel('alternating shear stress TAUa (ksi)')

xlim([0 250])

ylim([0 100])

Figure E13-02.3. Constructing the Modified-Goodman Diagram, completed.

6	Any other combination of mean and alternating stress with a stress ratio R >= 0 for this material and number of cycles can now be plotted on this diagram to obtain a safety factor.