EXAMPLE 6-1

Determining Estimated S-N Diagrams for Ferrous Materials

Problem	Create an estimated S-N diagram for a bar and define its equations.  How many cycles of life can be expected if the alternating stress is 100 MPa?

Given	The bar is square and has a hot-rolled finish.  The loading is fully reversed bending.

Tensile strength

Sut = 600;   % MPa

Maximum temperature

Tmax = 500;  %C

Bar side dimension

b = 150;     % mm

Alternating stress

SIGa = 100;  % MPa

Reliability

R = 0.999;

Assumptions	Infinite life is required and is obtainable since this ductile steel will have an endurance limit.  A reliability factor of 99.9% will be used.

Solution	See M--Book Ex06-1.doc and M-File Ex06_01.m.

1	Since no endurance-limit or fatigue strength information is given, we will estimate S'e based on the ultimate tensile strength using equation 6.6a.

Sprime_e = 0.5 * Sut    % MPa

Sprime_e =

300

2	The loading is bending so the load factor from equation 6.7a is

Cload = 1.0;

3	The part size is greater than the test specimen and the part is not round, so an equivalent diameter based on its 95% stressed area must be determined and used to find the size factor.  For a rectangular section in nonrotating bending, the A95 area is defined in Figure 6-25c and the equivalent diameter is found from equation 6.7d

A95 = 0.05 * b * b  % mm2

dequiv = sqrt(A95 / 0.0766) % mm

A95 =

1125

dequiv =

121.1886

and the size factor is found for this equivalent diameter from equation 6.7b, to be

Csize = 1.189 * dequiv^-0.097   % no units

Csize =

0.7466

4	The surface factor is found from equation 6.7e and the data in Table 6-3 for the specified hot-rolled finish.

Table 6-3 constants

A = 57.7;

b = -0.718;

Csurf = A * Sut^b   % no units

Csurf =

0.5841

5	The temperature factor is found from equation 6.7f :

Ctemp = 1 - 0.0058 * (Tmax - 450)

Ctemp =

0.7100

6	The reliability factor is taken from Table 6-4 for R = 0.999 and is

Creliab = 0.753;

7	The corrected endurance limit Se can now be calculated from equation 6.6:

Se = Cload * Csize * Csurf * Ctemp * Creliab * Sprime_e   % MPa

Se =

69.9397

Let

Se = 70     % MPa  (rounded)

Se =

70

8	To create the S-N diagram, we also need a value for the estimated strength Sm at 103 cycles based on equation 6.9 for bending loading.

Sm = 0.90 * Sut   % MPa

Sm =

540

9	The estimated S-N diagram is shown in Figure 6-34 with the above values of Sm and Se.  The expressions of the two lines are found from equations 6.10a through 6.10c assuming that Se begins at 106 cycles.

b = (-1/3) * log10(Sm / Se)    % no units

a = Se / 10^(6*b)   % MPa

b =

-0.2958

a =

4.1657e+003

Plotting Sn as a function of N from equation 6.10a

N = 1000:10000:1e6;

Sn = a .* N.^b;   % MPa

FailLine = 100 * ones(size(Sn));

loglog(N,Sn,N,FailLine,'LineWidth',2)

grid on

xlabel('Number of cycles, N')

ylabel('Fatigue strength, Sn (MPa)')

FIGURE 6-34. S-N Diagram and Alternating Stress Line Showing Failure Point

10	The number of cycles of life for any alternating stress level can now be found from equation 6.10a by replacing σa for Sn.

At N = 103 cycles,

Sn3 = a * 1000^b   % MPa

Sn3 =

540.0000

At N = 106 cycles,

Sn6 = a * 1e6^b   % MPa

Sn6 =

70.0000

N = (SIGa / a)^(1/b)    % cycles

N =

2.9941e+005

The figure above shows the intersection of the alternating stress line (σa = 100 MPa) with the failure line at N = 3.0 x 105 cycles.