EXAMPLE 6-2

Determining Estimated S-N Diagrams for Nonferrous Materials

Problem	Create an estimated S-N diagram for an aluminum bar and define its equations.  What is the corrected fatigue strength at 2E7 cycles?

Given	The forged 6061-T6 bar is round.  The loading is fully reversed torsion.

Tensile strength

Sut = 45;    % ksi (ksi = 1000 psi)

Maximum temperature

Tmax = 300;  %F

Bar diameter

d = 1.5;     % in

Reliability

R = 0.999;

Assumptions	A reliability factor of  99.0% will be used.  The uncorrected fatigue strength will be taken at 5E8 cycles.

Solution	See M-Book Ex06-2.doc and M-File Ex06_2.m.

1	Since no fatigue strength information is given, we will estimate S'f based on the ultimate tensile strength using equation 6.5c.

Sprime_f = 0.4 * Sut    % ksi

Sprime_f =

18

This value is at N = 5E8 cycles.  There is no knee in an aluminum S-N curve.

2	The loading is pure torsion so the load factor from equation 6.7a is

Cload = 1.0;

because the applied torsional stress will be converted to an equivalent von Mises normal stress for comparison to the S-N strength.

3	The part size is greater than the test specimen and it is round, so the size factor can be estimated with equation 6.7b, noting that this relationship is based on steel data:

Csize = 0.869 * d^-0.097   % no units

Csize =

0.8355

4	The surface factor is found from equation 6.7e and the data in Table 6-3 for the specified forged finish, again with the caveat that these relationships were developed for steels and may be less accurate for aluminum.

Table 6-3 constants

A = 39.9;

b = -0.995;

Csurf = A * Sut^b   % no units

Csurf =

0.9037

5	Equation 6.7f  is for steel only so we will assume :

Ctemp = 1

Ctemp =

1

6	The reliability factor is taken from Table 6-4 for R = 0.990 and is

Creliab = 0.814;   % from Table 6.4

7	The corrected endurance limit Se can now be calculated from equation 6.6:

Sf = Cload * Csize * Csurf * Ctemp * Creliab * Sprime_f   % ksi

Sf =

11.0627

8	To create the S-N diagram, we also need a value for the estimated strength Sm at 103 cycles based on equation 6.9.  Note that the bending value is used for torsion.

Sm = 0.90 * Sut   % ksi

Sm =

40.5000

9	The coefficient and exponent of the corrected S-N line and its equation are found using equations 6.10a through 6.10c.  The value of z is taken from Table 6-5 for Sf at 5E8 cycles.

z = 5.699;

b = (-1/z) * log10(Sm / Sf)    % no units

a = Sm / 10^(3*b)   % ksi

b =

-0.0989

a =

80.1927

10	The fatigue strength at the desired life of N = 2 . 107 cycles can now be estimated from the equation for the corrected S-N line:

N = 2e7;

Sn = a * N^b   % ksi

Sn =

15.2094

Sn is larger than Sf because it is at a shorter life than the published fatigue strength.

11	Note the order of operations. We first found an uncorrected fatigue strength, Sf, at some "standard" cycle life (N = 5E8), then corrected it for the appropriate factors from equations 6.7.  Only then did we create equation 6.10a for the S-N line so that it passes through the corrected Sf at N = 5E8.  If we had created equation 6.10a using the uncorrected S'f, solved it for the desired cycle life (N = 2E7), and then applied the correction factors, we would get a different and incorrect result.  Because these are exponential functions, superposition does not hold.